| Shanghai Horse Construction Product Data Sheet Edition 8.2.2020 |  |  |  |  |
| --- | --- | --- | --- | --- |
| HM-120 |  |  |  |
| High Performance Steel Plate Bonding Epoxy Adhesive |  |  |  |

| Description | HM-120 High Performance Steel Plate Bonding Epoxy Adhesive is two-component, room temperature curing adhesive for externally bonded steel plate. |  |
| --- | --- | --- |
| Where to Use | Bonding steel plates to surfaces of beams, slabs, walls and columns for structural strengthening. |  |
| Advantages | ■ Thixotropic and non-sagging up to 2-3 cm thickness with lower hollow area. ■ Strong bond. ■ Suitable for most substrates. ■ High percentage of effective ingredients. ■ Fatigue and impact resistance. ■ High shear strength. ■ High durability. ■ Good resistance to water. ■ Appropriate curing time, easy handling within a wide range of temperatures. ■ Uniform mixing without bubbles. |  |
| Packaging | Component A: 20kg/barrel | Component B: 10kg/barrel |

Typical Data

| Shelf Life | 12 months in original, unopened containers |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Storage Conditions | Store dry at -5 °C ~ 40 °C |  |  |  |  |
| Color | Component A: Grey paste |  |  | Component B: Brown paste |  |
| Mixing Ratio | Component A: Component B =2: 1 by weight |  |  |  |  |
| Pot Life | Spring & Fall (23 °C) |  | Summer (30 °C) |  | Winter (10 °C) |
|  | ≥50 min |  | ≥40 min |  | 50~180 min |
| Tack-Free Time | Approximately 2 hours |  |  |  |  |
| Glass Transition Temperature (Tg) |  | 70 °C |  |  |  |
| Density |  | 1.8 ± 0.1 g/cm³ |  |  |  |
| Thixotropic Index (TI) |  | ≥4.0 |  |  |  |

Mechanical Properties

| Property |  | Test Method (GB50728-2011) |
| --- | --- | --- |
| Tensile Strength | ≥35 MPa | @ (23 ± 2) °C, (50 ± 5) % R.H. |
| Tensile Modulus | ≥5000 MPa |  |
| Tensile Elongation | ≥1.2% |  |
| Bending Strength | ≥50 MPa |  |
| Compressive Strength | ≥80 MPa |  |
| Metal-Metal Lap Shear Strength | ≥22 MPa |  |
| Metal-Metal Tensile Bond Strength | ≥36 MPa |  |
| Metal-Concrete Bond Strength | ≥2.5 MPa, and C60 concrete damage |  |
| Heat Deflection Temperature (HDT) | ≥65 °C | 21 days Constant bending load of 0.45 MPa |
| Non-volatile Matter | ≥99% | @ (105 ± 2) °C, (50 ± 5) min |

Long-term performance

| Environmental Resistance | Loss of shear strength | Test Method (GB50728-2011) |
| --- | --- | --- |
| Moist-Heat Resistance | ≤12% | 90 days, @ 50 °C, 90 % R.H. Compared with the short-term results at room temperature |
| Heat Aging Resistance | ≤5% | 30 days, @ (80 ± 2) °C Compared with the 10 min short-term results at the same temperature |
| Freeze-Thaw Resistance | ≤5% | -25°C ⇌ 35 °C, 8 hours per cycle, 50 cycles Compared with the short-term results at room temperature |

| Stress Resistant |  | Test Method (GB50728-2011) |
| --- | --- | --- |
| Long-term Stress Resistance | No shear damage in Metal-Metal Lap Shear Test. Creep deformation ≤0.4 mm | 210 days, @ (23 ± 2) °C, (50 ± 5) % R.H. Shear stress of 4.0 MPa |
| Fatigue Resistance | No shear damage in Metal-Metal Lap Shear Test under cyclic sine wave loading. | 2×106 cycles at room temperature Stress ratio of 5:1 Maximum stress of 4.0 MPa Cycling frequency of 5 Hz |

Corrosion resistance performance

| Corrosion resistance |  |  | Test Method (GB50728-2011) |
| --- | --- | --- | --- |
| Salt Spray Resistance | Loss of shear strength ≤5% | No cracks or degumming | Metal-Metal Lap Shear Test |
| Alkaline resistance | Concrete damage | No cracks, peeling or blistering | Metal-Concrete Bond Test |
| Acid resistance | Concrete damage | No cracks or degumming | Metal-Concrete Bond Test |

| Construction Process | Substrate treatment → Levelling → Lofting → Drilling location confirming → Bar planting → Steel plate treatment → Mixing → Application → Steel bonding → Fixing and compressing → Curing → Protection treatment |
| --- | --- |
| Attention | ■ Use necessary protective equipment (e.g., facemasks, gloves, goggles, etc.). ■ Take appropriate fire protection measures and keep work areas well ventilated. ■ Flush the skin immediately upon contaminated. ■ Seek emergency medical attention If the adhesive is accidentally swallowed or splashed into the eyes. |

For more information, please visit our website at www.horseen.com.